| 17.045 |  | Swing Arc |  |
| --- | --- | --- | --- |
| Size, mm: | 1300x5985x2465 | Weight, kg: | 240.279 |
| Material characteristics |  |  |  |
| General description of the design The product is a set of U-shaped frames with crossbars, a suspension with rope weaving and two suspensions on chains. Materials and components Powder-painted steel with a layer of zinc-containing primer, polypropylene reinforced rope, stainless steel fasteners. The metal is painted with anthracite gray polymer paint. The swing includes a “nest” suspension with a weighted rim. The diameter of the suspension is 1045 mm. The weaving inside the ring is made of four-strand reinforced rope with a diameter of 16 mm. The swing is equipped with suspensions made of four-strand reinforced rope. The swing is designed for intensive use, can withstand loads of up to 250 kg - suitable for playgrounds in public places (parks, squares, local areas). Metal parts are coated in two layers: a zinc-containing powder primer is applied as the first layer, which is a powder mixture based on epoxy resin, zinc and targeted additives, is polymerized in a high-temperature chamber. As a finishing layer, polyester powder paint is applied, which is a homogenized powder mixture of polyester resin, hardeners, pigments, fillers and modifiers selected to provide weather resistance and light resistance. The finishing layer is polymerized in a high-temperature chamber. Frame The frame consists of three supports, each of which is made of metal pipes and two crossbars fixed between them, made from round pipe 89x3mm. |  |  |  |