| 39.117 |  | Urn |  |
| --- | --- | --- | --- |
| Size, mm: | 400x500x700 | Weight, kg: | 150 |
| Material characteristics |  |  |  |
| Material: architectural concrete. Concrete compressive strength class: B25 Frost resistance grade: F 150 Water resistance grade: W 6 Composition: White Portland cement M-500 Filler: marble chips of fraction 5-10 mm. Front surface: smooth, polished, with the structure of natural stone. Type: monolithic structure. |  |  |  |